# PRODUCT SPECIFICATION

- PRODUCT CODE HMC04/0.75

- DESCRIPTION	3 Core + Earth 24/.2 (0.5mmsq). T.C.W. V90HT PVC insulated. White cores numbered V90HT P.V.C. sheathed.

Control cable. 450/750 volt to AS5000.3 Oxygen Free copper. RoHS compliant PVC.

# CONSTRUCTION

  - CONDUCTOR : 24 strands of 0.2 mm nom. Tinned Annealed Copper to

AS1125 drawn from Class 102 copper to AS1574.

Max. D.C. resistance at 20C : 26 ohms / km

  - INSULATION : White V90HT PVC to AS3808.

Nominal  Diameter:        2.35 mm Nominal Wall Thickness: 0.6 mm

  - LAY  UP	4 Cores laid up

1. White  No1	2. White  No2	3. White  No3      4. Green/Yellow

  - SHEATH	Coloured P.V.C. type V90HT  to AS3808.

Nominal  Diameter:	8.1 mm Nominal Wall Thickness:    1.15 mm

# IDENTIFICATION

Printed on sheath at approx. 500mm intervals

TYCAB 4 X 0.75MMSQ 2019 V90HT ELECTRIC CABLE 450/750V