# PRODUCT SPECIFICATION

- PRODUCT CODE HMC07/0.5

- DESCRIPTION	6 Core + Earth 16/.2 (0.5mmsq). T.C.W. V90HT PVC insulated. White cores numbered V90HT P.V.C. sheathed.

Control cable. 450/750 volt to AS5000.3 Oxygen Free copper. RoHS compliant PVC.

# CONSTRUCTION

  - CONDUCTOR : 16 strands of 0.2 mm nom. Tinned Annealed Copper to

AS1125 drawn from Class 102 copper to AS1574.

Max. D.C. resistance at 20C : 39 ohms / km

  - INSULATION : White V90HT PVC to AS3808.

Nominal  Diameter:	2.1 mm Nominal Wall Thickness: 0.6 mm

  - LAY  UP	7 Cores laid up

1. White  No1	2. White  No2	3.	 White  No3   4. White  No4               5. White  No5      6. White  No6     7. Green/Yellow

  - SHEATH	Coloured P.V.C. type V90HT  to AS3808.

Nominal  Diameter:	8.9 mm Nominal Wall Thickness:    1.25 mm

# IDENTIFICATION

Printed on sheath at approx. 500mm intervals

TYCAB 7 X 0.5MMSQ 2019 V90HT ELECTRIC CABLE 450/750V