PRODUCT SPECIFICATION

1. PRODUCT CODE:    	ATC52603

2. DESCRIPTION          	5 Core 23/.32 (1.84mm2).

Plain Copper Wire

V90 P.V.C. Insulated and 5V90 P.V.C. Sheathed Trailer cable.

Extra Low Voltage. Not for Mains connection.

RoHS compliant P.V.C.

Oxygen Free copper.

3. CONSTRUCTION

3.1 CONDUCTOR:	23 strands of 0.32 mm nom. Annealed Copper to AS/NZS1125

drawn from Class 102 copper to AS/NZS1574.

Max. D.C. resistance at 20C:		10.3 ohms / km

3.2 INSULATION:	Coloured V90 P.V.C. to AS/NZS3808.

Nominal Diameter:		2.6 mm

Nominal Wall Thickness:   		0.4 mm

3.3 LAY UP:                	5 Cores laid up.

1. Brown

2. Red

3. Green

4. White

5. Yellow

3.4 SHEATH:               	Coloured P.V.C. type 5V90 to AS/NZS3808.

Nominal Diameter:		8.2 mm

Nominal Wall Thickness:		0.6 mm

TYPICAL ROPY TRAILER CABLE FINISH