PRODUCT SPECIFICATION

1. PRODUCT CODE     	BEM27085

2. DESCRIPTION           	2 Core Flat Twin 7/0.85 (4mm2 nom.). P.A.C.W.                              		            				V90 Insulated and 3V90 P.V.C. Sheathed.

Building Cable 450/750 Volt to AS/NZS 5000.2.

Oxygen Free Copper. RoHS Compliant.

TUV AUTHORISED MARKING: TUV022085EA

3. CONSTRUCTION

3.1 CONDUCTOR:   	7 strands of 0.85 mm nom. Plain Annealed Copper to

AS/NZS 1125 Class 2.

Max. D.C. resistance at 20C: 	4.61 ohms / km

3.2 INSULATION:    	Coloured V90 P.V.C. to AS/NZS 3808.

Nominal Diameter:  		4.15 mm

Nominal Wall Thickness:   		0.8 mm

3.3 CORE COLOURS: 	1. RED

2. BLACK

Laid parallel

3.4 SHEATH:               	Coloured 3V90 P.V.C. to AS/NZS 3808.

Flat configuration

Nominal Dimensions:    		6.4 x 10.5 mm

Nominal Wall Thickness:    	1.1 mm

3.5 IDENTIFICATION:	Printed on the sheath at maximum distance of 550mm:

TYCAB  AUSTRALIA  2017  V90 ELECTRIC CABLE  450/750V TUV022085EA  BEM27085  2X4MM2

And Metre Marked